[image: image1.emf]HC-AA-010-050-XXX


Date


Singnature


       50  ohms 


Transmission Lines


HC----- Fidelics Microelectronics Code.


AA-----(Asfired)99.6


% AL


2


O


3.


010-----Substrate Thickness 0.010"(0.254mm)


050-----Circuit Width 0 .050"(1.27mm)


XXX-----Circuit Length "L"


 


specified by Customer.


         


 


Notes


  


Circuit No


:


HC-AA-010-050-XXX


1.Material: 0.010" THK Alumina 99.6


%


  Surface Finish


＜


4 Micoinches.


2.Metalizations


  Front side


 


Au Thickness :160 Micoinches


±


20


%.


  Back side Au Thickness 


＞


40 Micoinches


Technical Specification


99.6


% AL


2


O


3


REV NO


REV


Fidelics 


Microelectronics




HC-AA-010-050-XXX

Date Singnature

       50  ohms 

Transmission Lines

HC----- Fidelics Microelectronics Code.

AA-----(Asfired)99.6% AL

2

O

3.

010-----Substrate Thickness 0.010"(0.254mm)

050-----Circuit Width 0 .050"(1.27mm)

XXX-----Circuit Length "L"

 

specified by Customer.

          

Notes

  Circuit No:HC-AA-010-050-XXX

1.Material: 0.010" THK Alumina 99.6%

  Surface Finish＜4 Micoinches.

2.Metalizations

  Front side Au Thickness :160 Micoinches±20%.

  Back side Au Thickness ＞40 Micoinches

Technical Specification

99.6% AL

2

O

3

REV NO REV

Fidelics 

Microelectronics


