
[image: image1.wmf]Fidelics

Microelectronics

REV

REV NO

99.6% AL

2

O

3

Technical Specification

1.Material: 0.015" THK Alumina 99.6%

  Surface Finish

＜

4 Micoinches.

2.Metalizations

  Front side

 

Au Thickness :160 Micoinches

±

20%.

  Back side Au Thickness 

＞

40 Micoinches

         

 

Notes

  

Circuit No

:

HC-AA-015-050-XXX

HC----- Fidelics Microelectronics Code.

AA-----(Asfired)99.6% AL

2

O

3.

015-----Substrate Thickness 0.015"(0.381mm)

050-----Circuit Width 0 .050"(1.27mm)

XXX-----Circuit Length "L"

 

specified by Customer.

       50  ohms

Transmission Lines

Singnature

Date

HC-AA-015-050-XXX


_1309239111.dwg

